## Slide 1: In_situ_STXM-chemi-movies: CO2R@ Bessy-II
Chunyang Zhang, Haytham Eraky, Matt Gibson, Adam Hitchcock, Drew Higgins (McMaster University); Markus Weigand, Thomas Rauch, Xianxiao Sun (Bessy-II);
Cu-CO2R_in_situ_STXM-movies-BessyII-Feb23.ppt 07 May 2023 (aph)
Goals: in-situ STXM movie and CO2R
Expt:Record repetitive 4-E stacks on the in situ Cu(0)/Cu(1) system after it was switched to CO2-saturated KHCO3. The first 3 were sampling during 3 slow cv’s (2 mV/s, or 1 mV/s). The last was Linear scan voltammetry from 0 to -0.8 Vau corresponding to converting from electrodeposition to CO2 reduction
Bessy-II
04/05 Feb 2023
Results:
In-situ STXM chemical movies show
changes of Cu oxidation states during scan
120
-20
nm
Cu(I)
40
-55
Cu(II)
Cu(0)
30
-5
d
e
f
Initial state (0 VAu)
120
0
30
0
30
0
nm
145
0
20
0
20
0
Final state
( -0.8 VAu)
Scan rate = 0.2 mV/s
a
b
c
Display as slide show to view movies